

**Natural Wear60 Rubber**

Our Natural Wear60 Abrasion Resistant rubber has similar properties to BS1154 Natural Rubber.

Please see below comparison chart:

|  |  |  |
| --- | --- | --- |
| **Properties** | **BS1154**  | **NZ Rubber Wear60**  |
| **Product** | Natural Rubber | Natural Rubber |
| **Colour** | Black | Black |
| **Compound** | NR | NR |
| **Hardness (ShoreA)** | 60° +/- 5 | 60° +/- 5 |
| **Density** | 1.2g/cm³ | 1.13g/cm³ |
| **Tensile Strength** | 17Mpa | 15Mpa |
| **Elongation at Break** | 400% | 400% |
| **Abrasion Resistance** | 130mm³ | 150mm³ |
| **Temperature Range** | -20°c- +70°c | -30°c- +70°c |

Natural Wear60 Rubber is available in the following thicknesses:

1.5mm | 3mm | 4.5mm | 6mm | 10mm | 12mm | 16mm thick

Roll size is 1.2m wide x 10m long.

We can supply per/m or cut the rolls into your required width.