|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 65 +/-5 ShoreA |
| **Tensile Strength** | 7MPA |
| **Elongation** | 300% |
| **Surface** | Smooth |
| **Density** | 1.3g/cm³ |
| **Temperature Range** | -40°C – 110°C |



**Butyl Rubber**

* Gaskets
* Waterproofing