|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 35 +/-5 ShoreA |
| **Tensile Strength** | 3 MPA |
| **Elongation** | 368% |
| **Temperature Range** | -38°C to 120°C |
| **Surface** | Smooth |
| **Density** | 0.75cm³ |
| **Tear Strength** | 4.5 KN/M |



**D-Shape EPDM Sponge Seal**

* Designed for sealing against dust and water penetration
* High Density Closed Cell EPDM Sponge
* UV Stable
* Self-Adhesive Backing