|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 65 +/-5 ShoreA |
| **Tensile Strength** | 3-4MPA |
| **Elongation** | 200% |
| **Surface** | Dimple Pattern |
| **Density** | 1.5g/cm³ |



**Dimple Matting**

* Horse Float & Truck Matting
* Stables
* Pits
* Trailers
* Gyms
* Doggy Daycares
* Commercial boats