|  |  |  |
| --- | --- | --- |
| **Colour** |  | Black/White |
| **Compression Set 25%** | ASTM D1056 | 40% |
| **Tensile Strength (kPa)** | ASTM D412 | 2.7 |
| **Elongation** | ASTM D412 | 150% |
| **Hardness** | ASTM D2240 | 18 +/-4 Shore C |
| **Compression Strength****25%** | ASTM D1056 | 35 kPa |
| **Density kg/m³** | ASTM D3575 | 120 +/-20 |
| **Tear Strength** | ASTM D624 | 2.7 kN/m |
| **Temperature Rating** |  | -20°c - +90°c |



**EPDM Foam Sheet (Black/White)**

Note: Sulphur Free