|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 35 +/-5 ShoreA |
| **Tensile Strength** | 2.8 MPA |
| **Elongation** | 360% |
| **Temperature Range** | -38°C to 120°C |
| **Surface** | Smooth |
| **Density** | 0.65 – 0.85g/cm³ |



**EPDM Sponge Seal**

* Designed for sealing against dust and water penetration
* High Density Closed Cell EPDM Sponge
* UV Stable