|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 50 +/-5 ShoreA |
| **Tensile Strength** | 3MPA |
| **Elongation** | 200% - 250% |
| **Temperature Range** | -10°C to 60°C |
| **Surface** | Smooth |
| **Density** | 1.5g/cm³ |



**Natural Rubber IRHD50/55**

* Conveyor Skirting Rubber