|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 60 +/-5 ShoreA |
| **Tensile Strength** | 4MPA |
| **Elongation** | 120% - 180% |
| **Temperature Range** | -50°C to 110°C |
| **Surface** | Smooth |
| **Density** | 1.6g/cm³ |



**Natural Rubber IRHD60**

* Gaskets