|  |  |  |
| --- | --- | --- |
| **Colour** |  | Black |
| **Hardness** | ASTMD2240 | 60 +/-5 ShoreA |
| **Tensile Strength** | ASTMD-412 | 15MPA |
| **Elongation** | ASTMD-412 | 400% |
| **Surface** |  | Smooth |
| **Density** | ASTMD792 | 1.13g/cm³ |
| **Abrasion** | ASTMD-412 | 150 mm³ |
| **Temperature Range** |  | In Air: -30°C – +70°CWater: -30°C – +80°C |



**Natural Wear Rubber 60 SHoreA**

Natural Rubber (NR) also called pure gum rubber is used in a wide range of industries. NR rubber has excellent mechanical properties, low compression set and high resilience. It has excellent dynamic and rebound properties and very good resistance to abrasion.

**Main Characteristics:**

**Elasticity:** Excellent

**Compression:** Excellent

**Abrasion:** Excellent

**Flame:** Poor

**Fuels:** Unsuitable

**Ozone:** Unsuitable