|  |  |
| --- | --- |
| **Colour** | Black |
| **Compression Set** | 90.8% |
| **Tensile Strength** | 5.1 kgf/cm³ |
| **Elongation** | 237% |
| **Tearing** | 2.0 kgf/cm³ |
| **Surface** | Plain both sides |
| **Density** | 1.6g/cm³ |
| **Temperature Range** | -20°c - +90°c |



**Neoprene Foam**