|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 60 +/-5 ShoreA |
| **Tensile Strength** | 5MPA |
| **Elongation** | 150% - 200% |
| **Temperature Range** | -30°C to 120°C |
| **Surface** | Smooth |
| **Density** | 1.5g/cm³ |



**Neoprene Rubber**

* Good resistance to Grease and Oil
* Good ozone and U.V. resistance
* Suitable for outdoor applications
* Gaskets
* Baffles
* Joint Sealing
* Bearing Rubber