|  |  |
| --- | --- |
| **Colour** | Black / White |
| **Hardness** | 60 +/-5 ShoreA |
| **Tensile Strength** | 3MPA |
| **Elongation** | 150% - 200% |
| **Temperature Range** | -30°C to 120°C |
| **Surface** | Smooth |
| **Density** | 1.5g/cm³ |



**Nitrile Rubber 30%**

* Good resistance to Grease and Oil
* Gaskets
* Drain Mats