|  |  |
| --- | --- |
| **Colour** | Black  |
| **Hardness** | 65 +/-5 ShoreA |
| **Tensile Strength** | 10MPA |
| **Elongation** | 350% |
| **Temperature Range** | -25°C to 70°C |
| **Surface** | Smooth |
| **Density** | 1.3g/cm³ |



**Nitrile Rubber 70%**

* Good resistance to Grease and Oil
* Good resistance to Petrol and Diesel
* Gaskets