|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 65 +/-5 ShoreA |
| **Tensile Strength** | 3MPA |
| **Elongation** | 200% |
| **Surface** | Smooth |
| **Density** | 1.5g/cm³ |
| **Temperature Range** | -10°C – 70°C |



**30% Nitrile Rubber with Cloth Insertion**