|  |  |  |
| --- | --- | --- |
| **Colour** |  | Charcoal |
| **Compression Set**  **(Room temp 22hr)** | ASTM D395-03 | 27 |
| **Tensile Strength** | ASTM D412-06a | 2.8 kgf/cm³ |
| **Elongation** | ASTM D412-06a | 76% |
| **Compressive Strength**  **(kgf/cm³ x 10% Strain)** | ASTMD1621-04a | 5.1 |
| **Surface** |  | Plain both sides |
| **Density** | ASTM C303-07 | 27g/cm³ |
| **Water Absorption**  **(%) 23°C, 24hr)** | ASTM C272-01 | 3.9% |



**PE Foam Tubes**