|  |  |
| --- | --- |
| **Colour** | Clear/White |
| **Hardness** | 60 +/-5 ShoreA |
| **Tensile Strength** | 6MPA |
| **Elongation** | 300% |
| **Temperature Range** | -50°C to 200°C |
| **Surface** | Smooth |
| **Density** | 1.25g/cm³ |



**Silicone Rubber**

* Gaskets
* Heat Sealing Equipment