|  |  |
| --- | --- |
| **Colour** | Black |
| **Hardness** | 75 +/-5 ShoreA |
| **Tensile Strength** | 6.5MPA |
| **Elongation** | 150% |
| **Temperature Range** | -20°C to 200°C |
| **Surface** | Smooth |
| **Density** | 1.9g/cm³ |



**Viton Rubber**

* Very high quality synthetic rubber
* Good resistance to hydrocarbons
* High temperature resistance
* Resistant to aggressive chemicals