|  |  |
| --- | --- |
| **Colour** | White |
| **Hardness** | 65 +/-5 ShoreA |
| **Tensile Strength** | 3MPA |
| **Elongation** | 200% - 250% |
| **Surface** | Smooth |
| **Density** | 1.5g/cm³ |



**White EPDM Food Grade**

* FDA Approved (certificates available)
* Gaskets